### How to Print PA6-CF (Nylon 6 Carbon Fiber) Filament

- Printer Requirements:

  - Use a hardened steel or ruby-tipped nozzle to withstand carbon fiber abrasiveness.

  - An enclosed printer is recommended to prevent warping.

  - Use a direct drive extruder for better control, though high-quality Bowden setups can also work.

- Recommended Print Settings:

  - Nozzle Temperature: 260–290°C (Check manufacturer specs)

  - Bed Temperature: 70–110°C

  - Layer Height: 0.4 mm or greater (due to fiber size)

- Print Surface & Adhesion:

  - Use PEI.

  - Apply a glue stick or a PA-specific adhesive to prevent sticking too hard or warping.

- Drying the Filament:

  - Critical step – Nylon is extremely hygroscopic.

  - Dry filament at 80-90°C for 12 hours before printing.

  - Check for <20% relative humidity before printing.

  - Store in a dry box or vacuum-sealed bag with desiccant.

- Speed & Retraction:

  - Print Speed: 60 mm/s (slower for better quality)

  - Retraction: 1–2 mm @ 20–40 mm/s (tune for your setup to avoid stringing)

- Notes

  - The body shrinks enough to warrant printing at 1.01-1.02 scale.

  - For a looser battery cage fit, scale the print 0.98 - 0.99.

### How to Print PPA-CF (Carbon Fiber Reinforced Polythiazide) Filament

- Printer Requirements:

  - All-metal hotend rated for 320 °C or higher.

  - Hardened steel  nozzle required (carbon fiber is abrasive).

  - Nozzle size: 0.4 mm+ (0.6 mm preferred to reduce clogging).

  - Heated enclosure recommended to prevent warping.

- Recommended Print Settings:

  - Nozzle Temperature: 280–320 °C (check your specific brand).

  - Bed Temperature: 80–120 °C (with adhesive aid).

  - Layer Height: 0.1–0.25 mm (0.2 mm typical).

  - Cooling Fan: Off or very low (0–30%).

- Print Surface & Adhesion:

  - Works well on PEI or Garolite with glue stick, Magigoo PA, or PVA glue.

  - Use a brim or raft for better first-layer grip.

  - Keep bed clean and pre-heated before printing.

- Drying the Filament:

- PPA-CF is very hygroscopic; print only when dry.

- Dry at 100–130 °C for 8–12 h (or 70 °C for 18–24 h in a filament dryer).

- Store in a dry box or airtight container with desiccant.

- Aim for <15% relative humidity.

- Speed & Retraction:

- Print Speed: 30–80 mm/s (slower for fine detail).

- Retraction: 0.5–1.5 mm @ 25–40 mm/s.

- Keep retractions minimal to avoid clogging.

Optional Post-Processing:

- Anneal printed parts at 80–100 °C for 4–12 h to improve strength and heat resistance.

### How to Print TPU (Thermoplastic Polyurethane) Filament

- Printer Requirements:

  - Direct drive extruder is highly recommended – TPU is flexible and can jam in Bowden tubes. 95A should be fine.

  - Use a printer with a fully constrained filament path to prevent buckling.

  - Works well on open-frame printers – no enclosure required.

- Recommended Print Settings:

  - Nozzle Temperature: 210–240°C (check your specific TPU brand)

  - Bed Temperature: 30–60°C (optional; helps first-layer adhesion)

  - Layer Height: 0.1–0.3 mm (0.2 mm is typical)

- Print Surface & Adhesion:

  - Sticks well to PEI.

  - Use a brim or skirt to help with initial adhesion and oozing control.

- Drying the Filament:

  - TPU is hygroscopic; it absorbs moisture easily.

  - Dry at 40–50°C for 12 hours before printing.

  - Check for <20% relative humidity before printing.

  - Store in a dry box or airtight container with desiccant.

- Speed & Retraction:

  - Print Speed: 15–60 mm/s (go slow to avoid issues)

  - Retraction: Minimal (0.5–2 mm @ 10–25 mm/s); too much can cause clogs or jams

  - Enable avoid crossing walls.

  - Disable coasting, combing, and z-hop for more consistent extrusion

### How to Remove Supports from 3D Prints

- Let the Print Cool First:

  - Allow the print to cool fully before handling—supports are easier to break off cleanly when the material is rigid.

- Start with Your Hands:

  - Gently break away large support structures by hand.

  - Flex the part slightly (if it's not brittle) to loosen supports from internal cavities.

  - Be sure to support small features when removing supports.

- Use the Right Tools:

  - Flush cutters or diagonal pliers for precise nips

  - Deburring tool or X-Acto knife for edge cleanup

  - Needle-nose pliers for tight or internal areas

  - Tweezers for stringy supports in fine details

- Use Support Interface Layers (Slicer Tip):

  - When slicing, enable support interface layers (denser contact layers) for easier, cleaner breakaway.

  - Consider "air gap" settings for easier removal—typically 0.2 mm for PLA, more for PETG or TPU.

- Print Orientation Matters:

  - Orient parts to minimize supports or make them easier to remove (e.g., flat surfaces facing down).

- Stay Safe:

  - Wear gloves and eye protection when using sharp tools.

  - Cut away from your body—many support injuries come from rushed removal.